Supplementary File

Rheological Optimization of Water-Based Mud Formulated with Carboxymethyl Hydroxypropyl Guar and Silica Nanoparticles

The obtained final coded and actual equations(vi to xiv) in terms of definite factors are given as follows:

AY= + 35.5  + 7.375A + 9.875B+ 0.375C -  4.9375A² - 9.4375B² -4.1875C²                                                                                                                                             (vi)

PV= + 15.736 + 4.375A +2.25B + 1.125C - 3.1578A² - 2.907B² (vii)

YP= + 31.863 + 5.487A + 7.25B + 1.987C -5BC - 4.592A² - 8.067B²        (viii)

GS 10 sec= + 14+ 3.125A + 2B + 1.375C - 1.36 BC - 2.625A2- 2.375B2-1.125C²  (ix)

GS 10 min= + 16 + 3.5A + 1.875B + 1.375C -1BC - 2.75A² -2.5B² - 1.5C²  (x)

AV= -24.048 + 23CMHPG + 4.592BENTONITE + 17.5SNP - 8.777CMHPG² -0.116BENTONITE² -16.75SNP²                                                                                      (xi )

PV = -4.7 + 14.2CMHPG + 1.32BENTONITE + 2.25SNP-5.61CMHPG² - 0.035BENTONITE²                                                               (xii)

YP  =-23.02 + 19.56CMHPG + 4.34BENTONITE + 20.641SNP - 1.11BENTONITE × SNP-8.16CMHPG² - 0.09BENTONITE²                                                                           (xiii)

GS 10 SEC= -5.84 + 11.16CMHPG + 1.21BENTONITE + 10.58SNP - 0.22 BENTONITE × SNP -4.66CMHPG² - 0.02BENTONITE² - 4.5SNP²          (xiv)

GS 10 min=   -4.86 + 12CMHPG + 1.24BENTONITE +12.08SNP-0.22BENTONITE ×SNP- 4.88CMHPG² - 0.03BENTONITE² -6SNP²                                                   (xv)

Where A is CMHPG, B is Bentonite concentration, and C is SNP concentration.

Table S1. Box–Behnken design matrix showing coded and actual factor levels for the 17 experimental runs

| Run | Coded A (CMHPG) | Coded B (Bentonite) | Coded C (SNP) | Actual CMHPG (g) | Actual Bentonite (g) | Actual SNP (g) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | +1 | +1 | 0 | 1.50 | 24.00 | 0.50 |
| 2 | +1 | -1 | 0 | 1.50 | 6.00 | 0.50 |
| 3 | -1 | +1 | 0 | 0.00 | 24.00 | 0.50 |
| 4 | -1 | -1 | 0 | 0.00 | 6.00 | 0.50 |
| 5 | +1 | 0 | +1 | 1.50 | 15.00 | 1.00 |
| 6 | +1 | 0 | -1 | 1.50 | 15.00 | 0.00 |
| 7 | -1 | 0 | +1 | 0.00 | 15.00 | 1.00 |
| 8 | -1 | 0 | -1 | 0.75 | 15.00 | 0.00 |
| 9 | 0 | +1 | +1 | 0.75 | 24.00 | 1.00 |
| 10 | 0 | +1 | -1 | 0.75 | 24.00 | 0.00 |
| 11 | 0 | -1 | +1 | 0.75 | 6.00 | 1.00 |
| 12 | 0 | -1 | -1 | 0.75 | 6.00 | 0.00 |
| 13 | 0 | 0 | 0 | 0.75 | 15.00 | 0.50 |
| 14 | 0 | 0 | 0 | 0.75 | 15.00 | 0.50 |
| 15 | 0 | 0 | 0 | 0.75 | 15.00 | 0.50 |
| 16 | 0 | 0 | 0 | 0.75 | 15.00 | 0.50 |
| 17 | 0 | 0 | 0 | 0.75 | 15.00 | 0.50 |

Table S2. Models for summarized statistics and sequential models for a sum of squares were tested for rheological characteristics.

|  | Sum of squares | Df | Mean square | F-value | p-value | Std. Dev | R2 | Adj. R2 | Pred. R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (AV) |  |  |  |  |  |  |  |  |  |
| Mean | 12177.94 | 1 | 12177.94 |  |  |  |  |  |  |
| Linear | 1216.37 | 3 | 405.46 | 7.41 | 0.0038 | 3.2 | 0.9447 | 0.9115 | 0.7787 |
| 2FI | 22.19 | 3 | 7.40 | 0.1073 | 0.9539 | 8.30 | 0.6424 | 0.4278 | -0.0440 |
| Quadratic | 605.00 | 3 | 201.67 | 28.45 | < 0.0001 | 3.47 | 0.9447 | 0.9115 | 0.7787 |
| Cubic | 84.50 | 3 | 28.17 |  |  |  |  |  |  |
| Residual | 0.0000 | 4 | 0.0000 |  |  |  |  |  |  |
| Total | 14106.00 | 17 | 829.76 |  |  |  |  |  |  |
| (PV) |  |  |  |  |  |  |  |  |  |
| Mean | 2821.24 | 1 | 2821.24 |  |  |  |  |  |  |
| Linear | 203.75 | 3 | 67.92 | 8.17 | < 0.0001 | 2.88 | 0.9177 | 0.8804 | 0.7449 |
| 2FI | 7.25 | 3 | 2.42 | 0.2398 | 0.8666 | 3.17 | 0.6768 | 0.4829 | -0.0357 |
| Quadratic | 84.01 | 3 | 28.00 | 11.70 | < 0.0001 | 1.55 | 0.9463 | 0.8772 | 0.1404 |
| Cubic | 16.75 | 3 | 5.58 |  |  |  |  |  |  |
| Residual | 0.0000 | 4 | 0.0000 |  |  |  |  |  |  |
| Total | 3133.00 | 17 | 184.29 |  |  |  |  |  |  |
| (YP) |  |  |  |  |  |  |  |  |  |
| Mean | 11408.95 | 1 | 11408.95 |  |  |  |  |  |  |
| Linear | 693.00 | 3 | 231.00 | 5.29 | 0.0133 | 6.61 | 0.5497 | 0.4458 | 0.1772 |
| 2FI | 101.35 | 3 | 33.78 | 0.7246 | 0.5601 | 6.83 | 0.6301 | 0.4082 | -0.4027 |
| Quadratic | 385.50 | 3 | 128.50 | 11.14 | <0.0001 | 3.40 | 0.9324 | 0.8918 | 0.5976 |
| Cubic | 80.75 | 3 | 26.92 |  |  |  |  |  |  |
| Residual | 0.0000 | 4 | 0.0000 |  |  |  |  |  |  |
| Total | 12669.56 | 17 | 745.27 |  |  |  |  |  |  |
| GS 10 sec |  |  |  |  |  |  |  |  |  |
| Mean | 2101.24 | 1 | 2101.24 |  |  |  |  |  |  |
| Linear | 125.25 | 3 | 41.75 | 7.28 | 0.0041 | 2.39 | 0.6270 | 0.5409 | 0.4197 |
| 2FI | 4.25 | 3 | 1.42 | 0.2016 | 0.8929 | 2.65 | 0.6483 | 0.4372 | 0.0265 |
| Quadratic | 64.01 | 3 | 21.34 | 23.90 | <0.0001 | 0.9449 | 0.9687 | 0.9285 | 0.4994 |
| Cubic | 6.25 | 3 | 2.08 |  |  |  |  |  |  |
| Residual | 0.0000 | 4 | 0.0000 |  |  |  |  |  |  |
| Total | 2301.00 | 17 | 135.35 |  |  |  |  |  |  |
| GS 10 min |  |  |  |  |  |  |  |  |  |
| Mean | 2795.53 | 1 | 2795.53 |  |  |  |  |  |  |
| Linear | 141.25 | 3 | 47.08 | 6.86 | 0.0052 | 2.62 | 0.6129 | 0.5235 | 0.4007 |
| 2FI | 4.50 | 3 | 1.50 | 0.1771 | 0.9095 | 2.91 | 0.6324 | 0.4118 | -0.0111 |
| Quadratic | 74.97 | 3 | 24.99 | 17.94 | 0.0011 | 1.18 | 0.9577 | 0.9033 | 0.3231 |
| Cubic | 9.75 | 3 | 3.25 |  |  |  |  |  |  |
| Residual | 0.0000 | 4 | 0.0000 |  |  |  |  |  |  |
| Total | 3026.00 | 17 | 178.00 |  |  |  |  |  |  |

Table S3. shows the variance analysis and the significance of the model's regression coefficients.

|  | Sum of Squares | Df | Mean Squares | F-value | P- value |  |
| --- | --- | --- | --- | --- | --- | --- |
| (AV) |  |  |  |  |  |  |
| Model | 1821.37 | 6 | 303.56 | 28.45 | < 0.0001 | Significant |
| A- CMHPG | 435.13 | 1 | 435.13 | 40.79 | < 0.0001 |  |
| B- Bentonite | 780.13 | 1 | 780.13 | 73.12 | < 0.0001 |  |
| C- SNP | 1.13 | 1 | 1.13 | 0.1054 | 0.7521 |  |
| A2 | 102.65 | 1 | 102.65 | 9.62 | 0.0112 |  |
| B2 | 375.02 | 1 | 375.02 | 35.15 | 0.0001 |  |
| C2 | 73.83 | 1 | 73.83 | 6.92 | 0.0251 |  |
| Residual | 106.69 | 10 | 10.67 |  |  |  |
| Lack of fit | 106.69 | 6 | 17.78 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Total Core | 1928.06 | 16 |  |  |  |  |
| Std. Dev | 3.27 | R² | 0.9447 |  |  |  |
| Mean | 26.76 | Adj R² | 0.9115 |  |  |  |
| C.V.% | 9.20 | Pred R² | 0.7787 |  |  |  |
| (PV) |  |  |  |  |  |  |
| Model | 286.12 | 5 | 57.22 | 24.55 | < 0.0001 | Significant |
| A- CMHPG | 153.13 | 1 | 153.13 | 65.68 | < 0.0001 |  |
| B- Bentonite | 40.50 | 1 | 40.50 | 17.37 | 0.0016 |  |
| C- SNP | 10.13 | 1 | 10.13 | 4.34 | 0.0613 |  |
| A2 | 42.11 | 1 | 42.11 | 18.06 | 0.0014 |  |
| B2 | 35.70 | 1 | 35.70 | 15.31 | 0.0024 |  |
| Residual | 25.64 | 11 | 2.33 |  |  |  |
| Lack of fit | 25.64 | 7 | 3.66 |  |  |  |
| Error Pure | 0.0000 | 4 | 0.0000 |  |  |  |
| Total Core | 311.76 | 16 | 0.9177 |  |  |  |
| Std. Dev | 1.53 | R² | 0.8804 |  |  |  |
| Mean | 12.88 | Adj.R² | 0.7449 |  |  |  |
| C.V.% | 8.85 | Pred.R² | 16.5725 |  |  |  |
| (YP) |  |  |  |  |  |  |
| Model | 1175.37 | 6 | 195.90 | 22.98 | < 0.0001 | Significant |
| A- CMHPG | 240.90 | 1 | 240.90 | 28.26 | 0.0003 |  |
| B- Bentonite | 420.50 | 1 | 420.50 | 49.33 | < 0.0001 |  |
| C- SNP | 31.60 | 1 | 31.60 | 3.71 | 0.0831 |  |
| BC | 100.00 | 1 | 100.00 | 11.73 | 0.0065 |  |
| A2 | 89.04 | 1 | 89.04 | 10.45 | 0.0090 |  |
| B2 | 274.77 | 1 | 274.77 | 32.24 | 0.0002 |  |
| Residual | 85.24 | 10 | 8.52 |  |  |  |
| Lack of fit | 85.24 | 6 | 14.21 |  |  |  |
| Error Pure | 0.0000 | 4 | 0.0000 |  |  |  |
| Total Core | 1260.61 | 16 |  |  |  |  |
| Std. Dev | 2.92 | R² | 0.9324 |  |  |  |
| Mean | 25.91 | Adj. R² | 0.8918 |  |  |  |
| C.V.% | 9.27 | Pred. R² | 0.5976 |  |  |  |
| GS 10 sec |  |  |  |  |  |  |
| Model | 193.26 | 7 | 27.61 | 38.23 | < 0.0001 | Significant |
| A- CMHPG | 78.13 | 1 | 78.13 | 108.17 | < 0.0001 |  |
| B- Bentonite | 32.00 | 1 | 32.00 | 44.31 | < 0.0001 |  |
| C- SNP | 15.13 | 1 | 15.13 | 20.94 | 0.0013 |  |
| BC | 4.00 | 1 | 4.00 | 5.54 | 0.0431 |  |
| A2 | 29.01 | 1 | 29.01 | 40.17 | 0.0001 |  |
| B2 | 23.75 | 1 | 23.75 | 32.88 | 0.0003 |  |
| C2 | 5.33 | 1 | 5.33 | 7.38 | 0.0237 |  |
| Residual | 6.50 | 9 | 0.7222 |  |  |  |
| Lack of fit | 6.50 | 5 | 1.30 |  |  |  |
| Error Pure | 0.0000 | 4 | 0.0000 |  |  |  |
| Total Core | 199.76 | 16 |  |  |  |  |
| Std. Dev | 0.8498 | R² | 0.9675 |  |  |  |
| Mean | 11.12 | Adj. R² | 0.9422 |  |  |  |
| C.V.% | 7.64 | Pred. R² | 0.7760 |  |  |  |
| GS 10 min |  |  |  |  |  |  |
| Model | 220.22 | 7 | 31.46 | 27.62 | < 0.0001 | Significant |
| A- CMHPG | 98.00 | 1 | 98.00 | 86.05 | < 0.0001 |  |
| B- Bentonite | 28.13 | 1 | 28.13 | 24.70 | 0.0008 |  |
| C- SNP | 15.13 | 1 | 15.13 | 13.28 | 0.0054 |  |
| BC | 4.00 | 1 | 4.00 | 3.51 | 0.0937 |  |
| A2 | 31.84 | 1 | 31.84 | 27.96 | 0.0005 |  |
| B2 | 26.32 | 1 | 26.32 | 23.11 | 0.0010 |  |
| C2 | 9.47 | 1 | 9.47 | 8.32 | 0.0181 |  |
| Residual | 10.25 | 9 | 1.14 |  |  |  |
| Lack of fit | 10.25 | 5 | 2.05 |  |  |  |
| Error Pure | 0.0000 | 4 | 0.0000 |  |  |  |
| Total Core | 230.47 | 16 |  |  |  |  |
| Std. Dev | 1.07 | R² | 0.9555 |  |  |  |
| Mean | 12.82 | Adj.R² | 0.9209 |  |  |  |
| C.V.% | 8.32 | Pred. R² | 0.5813 |  |  |  |