Supplementary Information

Fuel-rich ammonia catalytic combustion on gadolinium-doped ceria (GDC) supported copper oxide catalyst

Siqi Wanga, Haliru Ibrahim Muhammada, Ziqi Shena and Mingming Zhua,*

aFaculty of Engineering and Applied Sciences, Cranfield University, Bedford, MK43 0AL, United Kingdom

# S1. Parameters for catalytic performance evaluation

The NH3 and O2 conversion, as well as the N2 and NOx selectivities were calculated using the equations below:

| NH3 conversion: XNH3=n(NH3)in-n(NH3)outn(NH3)in | (S1) |
| --- | --- |
| Oxygen conversion: XO2=n(O2)in-n(O2)outn(O2)in | (S2) |
| N2 selectivity: SN2=n(NH3)in-n(NH3)out-2×n(N2O)out-n(NO)out-n(NO2)outn(NH3)in-n(NH3)out | (S3) |
| N2O selectivity: SN2O=n(NH3)in-n(NH3)out-2×n(N2)out-n(NO)out-n(NO2)outn(NH3)in-n(NH3)out | (S4) |
| NO selectivity: SNO=n(NH3)in-n(NH3)out-2×n(N2)out-2×n(N2O)out-n(NO2)outn(NH3)in-n(NH3)out | (S5) |
| NO2 selectivity: SNO2=n(NH3)in-n(NH3)out-2×n(N2)out-2×n(N2O)out-n(NO)outn(NH3)in-n(NH3)out | (S6) |

where n(i)in and n(i)out is the amount of gas i entering or exiting the system in moles (i = NH3, N2, N2O, NO, or NO2).

# S2. DFT calculations and the formation energy approach

The four-layer slab models used for the DFT calculations are presented in Figure S1.

Figure S1 Slab models of (a) CuO, (b) CuO/γ-Al2O3, and (c) CuO/GDC. Red spheres: oxygen atoms; Brown spheres: copper atoms; Grey spheres: aluminium atoms; Yellow spheres: cerium atoms; Green sphere: gadolinium atom.

The total energies of the isolated gas-phase N and O atoms were calculated to be -262.03 and -558.25 eV, respectively. The total energies of the isolated gas-phase N2 and O2 molecules were calculated to be -540.19 and -1125.2 eV, respectively. The DFT-calculated energies of the clean slabs, the slabs with the adsorbed atom, the adsorption energies, and their corresponding formation energies are summarised in Table S1. An example is also provided to explain how the adsorption energy is obtained and converted to the formation energy using the “formation energy approach” [1].

Table S1 DFT-calculated energies and their corresponding formation energies.

|  | Cu | CuO | CuO/Al2O3 | CuO/GDC |
| --- | --- | --- | --- | --- |
| Total energy of slab (eV) | -20,033.60 | -78,112.08 | -24,817.66 | -133,174.86 |
| Total energy of slab with adsorbed N atom (eV) | -20,327.41 | -78,381.22 | -25,087.58 | -133,445.16 |
| Total energy of slab with adsorbed O atom (eV) | -20,626.14 | -78,673.09 | -25,381.33 | -133,739.25 |
| Adsorption energy of N (eV) | -3.29 | -7.11 | -7.89 | -8.26 |
| Formation energy of N (eV) | 4.76 | 0.95 | 0.18 | -0.19 |
| Adsorption energy of O (eV) | -5.80 | -2.76 | -5.41 | -6.14 |
| Formation energy of O (eV) | -1.46 | 0.02 | -1.07 | -1.79 |

The following example shows how an adsorption energy (adsorption energy of N on the CuO/Al2O3 surface) is calculated and converted to its corresponding formation energy:

Adsorption energy of N on the CuO/Al2O3 surface is calculated using the equation below:

EadsN*CuO/Al2O3=UN*CuO/Al2O3-UCuO/Al2O3-UN=-25,087.58--24,817.66--262.03=-7.89 eV

where EadsN*CuO/Al2O3 is the adsorption energy of N on the CuO/Al2O3 surface, UN*CuO/Al2O3 is the DFT-calculated total energy of the CuO/Al2O3 slab with the adsorbed N atom, UCuO/Al2O3 is the DFT-calculated total energy of the clean CuO/Al2O3 slab, and UN the DFT-calculated total energy of the isolated gas-phase N atom.

To convert the adsorption energy to its corresponding formation energy, the reference energy of N is firstly calculated using the equation below:

RN=12×UN2=12×-540.19 eV= -270.1 eV

where RN is the reference energy of N and UN2 is the DFT-calculated total energy of the N2 molecule.

The formation energy of N on the CuO/Al2O3 surface is then calculated using the equation below:

EN*CuO/Al2O3=UN*CuO/Al2O3-UCuO/Al2O3-RN= -25,087.58--24,817.66 --270.1=0.18 eV

where EN*CuO/Al2O3 is the formation energy of N adsorbed on the CuO/Al2O3 surface, which is used as the input data for the microkinetic model.

# S3. Reaction pathway for the microkinetic model

The following elementary reactions were included in the microkinetic model. The partial pressures of the reactant gases (NH3 and O2) were set according to the desired Equivalence Ratio (ER).

| R1 | 'O2_g + *_s <-> O2*' |
| --- | --- |
| R2 | 'NH3_g + *_s <-> NH3*' |
| R3 | 'O2* + *_s <-> O* + O*' |
| R4 | 'NH3* + *_s <-> NH2-H* + *_s -> NH2* + H*' |
| R5 | 'NH2* + *_s <-> NH-H* + *_s -> NH* + H*' |
| R6 | 'NH* + *_s <-> N-H* + *_s -> N* + H*' |
| R7 | 'NH3* + O* <-> NH2-OH* + *_s-> NH2* + OH*' |
| R8 | 'NH2* + O* <-> NH-OH* + *_s -> NH* + OH*' |
| R9 | 'NH3* + OH* <-> NH2-H2O* + *_s -> NH2* + H2O_g + *_s' |
| R10 | 'NH2* + OH* <-> NH-H2O* + *_s -> NH* + H2O_g + *_s' |
| R11 | 'NH* + OH* <-> N-H2O* + *_s -> N* + H2O_g + *_s' |
| R12 | 'N* + N* <-> N-N* + *_s -> N2_g + 2*_s' |
| R13 | 'N* + O* <-> N-O* + *_s -> NO* + *_s' |
| R14 | 'N* + NO* <-> N-NO* + *_s -> N2O_g + 2*_s' |
| R15 | 'OH* + H* <-> OH-H* + *_s -> H2O_g + 2*_s' |
| R16 | 'OH* + OH* <-> OH-OH* + *_s -> H2O_g + O* + *_s' |
| R17 | 'H* + O* <-> O-H* + *_s -> OH* + *_s' |
| R18 | 'NO* <-> NO_g + *_s' |

# References

[1]	Medford AJ, Shi C, Hoffmann MJ, Lausche AC, Fitzgibbon SR, Bligaard T, et al. CatMAP: A Software Package for Descriptor-Based Microkinetic Mapping of Catalytic Trends. Catal Letters 2015;145:794–807. https://doi.org/10.1007/s10562-015-1495-6.